1032NM PARTIAL REFLECTION MIRROR

(PARTIAL REFLECTION AT 1030-1070NM)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| G G1. G2. G3 G4 G5 |  | Partial Reflection Mirrors(High Energy) 1032nm; R98% Substrate: Fused Silica Diameter: 1" -0.20/+0.00 Fine polished – double side: Flatness: 10 / @ 633nm over aperture Surface quality: better than 20-10 S/D coated High energy dielectric coating ## PR @ 1030 -1070nm R = 98% 0o AOI; Center @1032nm Designed Surface -1(S1): CONCAVE Partial reflection coating, 0o AOI DESIGNED R = 98% @ 1032nm Surface -2(S2): FLAT AR @ 1030-1070nm (R<0.2%) Including: ROC -50mm P/N: PPRM10-1032-R98-N50 ROC -100mm P/N: PPRM10-1032-R98-N100 ROC -200mm P/N: PPRM10-1032-R98-N200 ROC -500mm P/N: PPRM10-1032-R98-N500 ROC -1000mm P/N: PPRM10-1032-R98-N1000 |  | AR COATED AT 1030-1070NM Thk > 2mm S2: FLAT S1: CONCAVE |