1064NM FLAT & CONCAVE HIGH REFLECTION MIRROR

ROC = -900, -1000, -2000, -3000, -4000, -5000, -  mm

(Option: short ROC = -100, -300mm available)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |
| --- | --- | --- | --- |
| M. M1. M2. M3 M4 M5 M6 M7 M8 M9 |  | 1064nm High Reflection Mirror (ROC: DIFFERENT) - Plano-concave, Fused silica; Thickness: T=6mm, 0.05mm - Surface 1 (S1): flat or concave Surface quality: 20-10 scratch/dig Coating: HR @1064nm(R>99.5%) 0o AOI, single surface coating S1: FLAT OR CONCAVE - Surface 2 (S2): flat, ground and uncoated A: Diameter:  12.7mm, 0.05mm; ROC: -900, -1000, -2000, -3000, -4000, -5000mm and Flat FLAT (R=), P/N: PHRM1064-PP-05 S1: Concave(R=-900), P/N: PHRM1064-PCV-05-N900 S1: Concave (R=-1000), P/N: PHRM1064-PCV-05-N1000 S1: Concave(R=-2000), P/N: PHRM1064-PCV-05-N2000 S1: Concave(R=-3000), P/N: PHRM1064-PCV-05-N3000 S1: Concave(R=-4000), P/N: PHRM1064-PCV-05-N4000 S1: Concave(R=-5000), P/N: PHRM1064-PCV-05-N5000 B: Diameter: 25.4mm, 0.05mm; Thk: 6mm S1:Concave(R= -300), P/N: PHRM1064-PCV-10-N300 C: Diameter: 25.4mm, 0.05mm; Thk: 3mm S1:Concave(R= -100), P/N: PHRM1064W-PCV-10-N100 (Wideband HR coating: 950 – 1150nm, 0-deg AOI) | ## HR @1064nm GROUND UNCOATED Thk=6mm S2: FLAT |