1550NM, C-BAND FLAT HIGH REFLECTION MIRROR & OUTPUT COUPLER

FLAT DEGISN; UV FUSED SILICA

| ITEM | QTY | PART NO./DESCRIPTIONS |  |
| --- | --- | --- | --- |
| J. J1 J2 J3 J4 J5 J6 J7 J8 J9 |  | 1550nm/C-Band High Reflection Mirror & Output Coupler - Plano-plano, UV Fused silica - Surface quality: 20-10 scratch/dig; - Flatness: /10 over aperture - Parallelism: < 3” DIELECTRIC COATING: - Surface 1 (S1) Coating: R @1550  30nm 0o AOI, - Surface 2 (S2): AR @ 1550  30nm A: Dia: 15.0, -0.2/+0.0mm; Thickness: T =1.000.05mm R >99.9% High Reflection, P/N: POC1550-PP-15/1-HR R =86%, P/N: POC1550-PP-15/1-R86 R=22%, P/N: POC1550-PP-15/1-R22 R=14%, P/N: POC1550-PP-15/1-R14 B: Dia: 15.0, -0.2/+0.0mm; Thickness: T =2.000.05mm R = 95%, P/N: POC1550-PP-15/2-R95 R = 90%, P/N: POC1550-PP-15/2-R90 R = 85%, P/N: POC1550-PP-15/2-R85 C: Dia: 12.7, -0.2/+0.0mm; Thickness: T =2.000.05mm R = 50%, P/N: POC1550-PP-12.7/2-R50 R = 55%, P/N: POC1550-PP-12.7/2-R55 | ## R @1550 30nm AR @ 1550  30nm S2: FLAT S1: FLAT 15mm 1” and 0.5” 1”Adaptor (c.w retaining ring) available in stock |