355+532+1064NM FLAT HIGH REFLECTION MIRROR

(HIGH REFLECTION AT 355/532/1064NM)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| H. H1. H2. H3 |  | High Reflection Mirrors(High Energy) Substrate: Fused Silica Fine polished – single side: Flatness: 10 / @ 633nm over aperture Surface quality: better than 20-10 S/D High energy dielectric coating High reflection coating, 0o AOI HR @ 355nm (R > 99.5%) HR @ 532nm (R > 99.8%) HR @ 1064nm (R > 99.8%) Back surface: ground Including: Diameter: 15mm (-0.20, +0.00mm); Thickness: 3mm (+/-0.10mm); P/N: PHRM-355310-PP-15/3 Diameter: 12.7mm(-0.20, +0.00mm);; Thickness: 6mm (+/-0.10mm); P/N: PHRM-355310-PP-12.7/6 Diameter: 25.4mm(-0.20, +0.00mm);; Thickness: 6mm (+/-0.10mm); P/N: PHRM-355310-PP-25.4/6 | ## HR @ ## 355nm 532nm ## 1064nm | GROUND UNCOATED Thk=3mm, 6mm S2: FLAT S1: FLAT |