355+532+1064NM FLAT HIGH REFLECTION MIRROR

(HIGH REFLECTION AT 355/532/1064NM)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| H. H1. H2. H3 |  | High Reflection Mirrors(High Energy) Substrate: Fused Silica Fine polished – single side: Flatness: 10 (/ @ 633nm over aperture Surface quality: better than 20-10 S/D High energy dielectric coating High reflection coating, 0o AOI HR @ 355nm (R > 99.5%) HR @ 532nm (R > 99.8%) HR @ 1064nm (R > 99.8%) Back surface: ground Including: Diameter: (15mm (-0.20, +0.00mm); Thickness: 3mm (+/-0.10mm); P/N: PHRM-355310-PP-15/3 Diameter: (12.7mm(-0.20, +0.00mm);; Thickness: 6mm (+/-0.10mm); P/N: PHRM-355310-PP-12.7/6 Diameter: (25.4mm(-0.20, +0.00mm);; Thickness: 6mm (+/-0.10mm); P/N: PHRM-355310-PP-25.4/6 |  |  |

# Text boxes

Thk=3mm, 6mm

GROUND

UNCOATED

S2: FLAT

## HR @

## 355nm

532nm

## 1064nm

S1: FLAT