| ITEM | QTY | PART NO./DESCRIPTION |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 1-A. |  | ### (A) Plano-Concave 1064nm Cavity Output Mirrors ### Plano-Concave design ### Material: BK 7 glass - Diameter: 25.4mm, -0.20,+0.00mm ### Edge Thickness: T > 2mm ### Surface quality: 20-10 scratch/dig ### SURFACE – 1: AR Coating ### AR @ 1064nm coating (T1 >99.8%); ### SURFACE – 2: Radius of Curvature: ### ROC-2 = 8-Type ROC ### - 25mm; - 50mm; - 100mm; - 200mm; ### - 300mm; - 500mm; - 800mm, - 1000mm ### Partial Reflection Coating & Quantity: - R21=60% @ 1064nm; QTY: 2pcs - R22=70% @ 1064nm; QTY: 2pcs - R23=80% @ 1064nm; QTY: 2pcs - R24=90% @ 1064nm; QTY: 2pcs - R25=92% @ 1064nm; QTY: 2pcs - R26=94% @ 1064nm; QTY: 2pcs - R27=98% @ 1064nm; QTY: 2pcs TOTAL: 112pcs for this Part (A). | Te D ### Surface – 2 ROC 2 = 8 types | - | ### Surface – 1 AR @1064nm at 0o AOI T1 > 99.8% ### D=25.4mm Te > 2mm |

| ITEM | QTY | PART NO./DESCRIPTION |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 1-B. |  | ### (B) Plano-Convex 1064nm Cavity Output Mirrors ### Plano-Convex design ### Material: BK 7 glass - Diameter: 25.4mm, -0.20,+0.00mm ### Edge Thickness: T > 2mm ### Surface quality: 20-10 scratch/dig ### SURFACE – 1: AR Coating ### AR @ 1064nm coating (T1 >99.8%); ### SURFACE – 2: Radius of Curvature: ### ROC-2 = 8-Type ROC ### + 25mm; + 50mm; + 100mm; + 200mm; ### + 300mm; + 500mm; + 800mm, + 1000mm ### Partial Reflection Coating & Quantity: R21=60% @ 1064nm; QTY: 2pcs Sub-Quantity: (Part B) 8 x (7 x 2pcs) + 7pcs = 119pcs - R22=70% @ 1064nm; QTY: 2pcs - R23=80% @ 1064nm; QTY: 2pcs - R24=90% @ 1064nm; QTY: 2pcs - R25=92% @ 1064nm; QTY: 2pcs - R26=94% @ 1064nm; QTY: 2pcs - R27=98% @ 1064nm; QTY: 2pcs 7-Type of Coating (8) DIA12.7mm & ROC=+800mm Plano-Convex Mirrors; 7-type coating; QTY: 1pc each – 7pcs TOTAL: 112+7=119pcs for this Part (B). | Te D ### Surface – 2 ROC 2 = 8 types |  | ### Surface – 1 AR @1064nm at 0o AOI T1 > 99.8% ### D=25.4mm Te > 2mm |

| ITEM | QTY | PART NO./DESCRIPTION |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 1-C. |  | ### (C) Plano-Plano 1064nm Cavity Output Mirrors ### Plano-Plano design ### Material: BK 7 glass - Diameter: 25.4mm, -0.20,+0.00mm ### Edge Thickness: T =6mm ### Surface quality: 20-10 scratch/dig ### SURFACE – 1: AR Coating ### AR @ 1064nm coating (T1 >99.8%); ### SURFACE – 2: Flat ### Partial Reflection Coating & Quantity: - R21=60% @ 1064nm; QTY: 2pcs - R22=70% @ 1064nm; QTY: 2pcs - R23=80% @ 1064nm; QTY: 2pcs - R24=90% @ 1064nm; QTY: 2pcs - R25=92% @ 1064nm; QTY: 2pcs - R26=94% @ 1064nm; QTY: 2pcs - R27=98% @ 1064nm; QTY: 2pcs - R28 > 99.9% @ 1064nm; QTY: 2pcs 8-Type of Coating - DIA12.7mm & ROC=+800mm Plano-Convex Mirrors; R>99.9%@ 1064nm(Convex)/AR @ 1064nm(flat); | Te D ### Surface – 2: FLAT |  | ### Surface – 1 AR @1064nm at 0o AOI T1 > 99.8% ### D=25.4mm Te = 2mm |