532+1064NM FLAT HIGH REFLECTION MIRROR

(HIGH REFLECTION AT 532/1064NM, DUAL-WAVELENGTH DESIGN)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| G. G1. G2. G3 |  | High Reflection Mirrors(High Energy) Substrate: Fused Silica Fine polished – single side: Flatness: 10 / @ 633nm over aperture Surface quality: better than 20-10 S/D High energy dielectric coating High reflection coating, 45o AOI DESIGNED HR @ 532nm (R > 99.8%) and HR @ 1064nm (R > 99.8%) Back surface: clear & uncoated Including: Diameter: 2" x 12mm;. P/N: PHRM-45-5310-PP-20 Diameter: 1" x 6mm; P/N: PHRM-45-5310-PP-10 Diameter: 0.5" x 6mm P/N: PHRM-45-5310-PP-05 | ## HR @ 532nm ## 1064nm 45o AOI | GROUND UNCOATED Thk=3mm, 6mm S2: FLAT S1: FLAT |