532+1064NM FLAT HIGH REFLECTION MIRROR

(HIGH REFLECTION AT 532/1064NM, DUAL-WAVELENGTH DESIGN)

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| G. G1. G2. G3 |  | High Reflection Mirrors(High Energy) Substrate: Fused Silica Fine polished – single side: Flatness: 10 (/ @ 633nm over aperture Surface quality: better than 20-10 S/D High energy dielectric coating High reflection coating, 45o AOI DESIGNED HR @ 532nm (R > 99.8%) and HR @ 1064nm (R > 99.8%) Back surface: clear & uncoated Including: Diameter: (2" x 12mm;. P/N: PHRM-45-5310-PP-20 Diameter: (1" x 6mm; P/N: PHRM-45-5310-PP-10 Diameter: (0.5" x 6mm P/N: PHRM-45-5310-PP-05 |  |  |

# Text boxes

Thk=3mm, 6mm

GROUND

UNCOATED

S2: FLAT

## HR @

532nm

## 1064nm

45o AOI

S1: FLAT