SELECTION GUIDE   								       latest update date: 02 July 2008

(IN STOCK; DELIVERY IMMEDIATELY FROM SINGAPORE STOCK)

(1) 493.5NM+780NM HIGH REFLECTION MIRROR - (TWO-WAVELENGTH COATING)

(TWO-SIDE DIELECTRIC COATED)

| ITEM | PART NO./DESCRIPTIONS | IN-STOCK QUANTITY | APPLICATION/DRAWING/COATING DESCRIPTIONS |
| --- | --- | --- | --- |
| 1. | 493.5nm & 780nm High-Reflection Mirrors(High Energy) Substrate: Fused Silica Diameter: 1” & 0.5" -0.20/+0.00; Thickness: 6.00±0.05mm Fine polished – double side: Flatness: / 10 @ 633nm over aperture Surface quality: better than 20-10 S/D coated High energy dielectric coating: 0o AOI DESIGNED Surface -1(S1): FLAT or CONCAVE R > 99.8% @ 493.5nm & 780nm Surface -2(S2): FLAT AR @ 493.5 & 780nm(R<0.2%) Including: |  | THK =6mm HR @ 493.5 & 780nm; R > 99.8%; 0o AOI; S1: FLAT or CONCAVE S2: FLAT AR @ 493.5 & @780nm |
| 1-1. | 0.5", Surface -1(S1): flat P/N: PM-05-HR493/780-AR-0-P | 48pcs | 02.Jul.2008 updated |
| 1-2 | 1", Surface -1(S1): flat P/N: PM-10-HR493/780-AR-0-P | 21pcs | 02.Jul.2008 updated |
| 1-3. | 0.5", Surface -1(S1): concave; ROC = - 50mm P/N: PM-05-HR493/780-AR-0-N50 | 20pcs | 02.Jul.2008 updated |
| 1-4 | 0.5", Surface -1(S1): concave; ROC = - 100mm P/N: PM-05-HR493/780-AR-0-N100 | 30pcs | 02.Jul.2008 updated |