SELECTION GUIDE   								       latest update date: 02 July 2008

(IN STOCK; DELIVERY IMMEDIATELY FROM SINGAPORE STOCK)

(1) 700~1150NM HIGH REFLECTION MIRROR  - (BROADBAND COATING 0O & 45O )

(SINGLE-SIDE DIELECTRIC COATED)

| ITEM | PART NO./DESCRIPTIONS | IN-STOCK QUANTITY | APPLICATION/DRAWING/COATING DESCRIPTIONS |
| --- | --- | --- | --- |
| 1. | 700~1150Nm High-Reflection Mirrors Substrate: Fused Silica Diameter: 0.5"/1"/2", ; Thickness: 3 ~ 6mm Fine polished – double side: Flatness: / 10 @ 633nm over aperture Surface quality: better than 40-20 S/D coated Full dielectric coating: both 0o & 45o AOI applicable Surface -1(S1): FLAT or CONCAVE R > 99% ave @ 700~1150nm Surface -2(S2): FLAT (uncoated/keep clear) Including: |  | 0o AOI 45o AOI Ø0.5, Ø1, Ø2”, x T SINGLE-SURFACE WIDEBAND HR COATING (0O & 45O) *HR coated on concave surface If with concave surface S1 S2 |
| 1-1. | 0.5" xT6mm; Surface -1(S1): flat P/N: PBB-05-R03 | 180pcs | 02.Jul.2008 updated |
| 1-2. | 1" xT6mm; Surface -1(S1): flat P/N: PBB-10-R03 | 70pcs | 02.Jul.2008 updated |
| 1-3 | 2" xT12mm; Surface -1(S1): flat P/N: PBB-20-R03 | 26pcs | 02.Jul.2008 updated |

Continued on Page 2 of 2

| ITEM | PART NO./DESCRIPTIONS | IN-STOCK QUANTITY | APPLICATION/DRAWING/COATING DESCRIPTIONS |
| --- | --- | --- | --- |
| 1-4. | 0.5" xT6mm; Surface -1(S1): concave; ROC = - 50mm P/N: PBB-05-R03-N50 | 11pcs (+ 9pcsREJ-samples) | 02.Jul.2008 updated |
| 1-5. | 1" xT5mm; Surface -1(S1): concave; ROC = - 50mm P/N: PBB-10-R03-N50 | 3pcs | 02.Jul.2008 updated |
| 1-6. | 1" xT3; Surface(S1): concave; ROC = - 36.28mm, EFL = -70mm P/N: PBB-10-R03-N36 | 2pcs | 02.Jul.2008 updated |
|  | 1" xT3; Surface(S1): concave; ROC = - 51.83mm, EFL = -100mm P/N: PBB-10-R03-N51 | -- |  |
| 1-7. | 1" xT3; Surface(S1): concave; ROC = - 64.79mm, EFL = -125mm P/N: PBB-10-R03-N64 | 1pc | 02.Jul.2008 updated |
| 1-8. | 1" xT3; Surface(S1): concave; ROC = - 77.75mm, EFL =-150mm P/N: PBB-10-R03-N77 | 1pc | 02.Jul.2008 updated |
| 1-9. | 1" xT3; Surface(S1): concave; ROC = - 90.70mm, EFL =-175mm P/N: PBB-10-R03-N90 | 1pc | 02.Jul.2008 updated |
| 1-10. | 1" xT3; Surface(S1): concave; ROC = - 103.66mm, EFL =-200mm P/N: PBB-10-R03-N103 | 1pc | 02.Jul.2008 updated |
| 1-11. | 1" xT3; Surface(S1): concave; ROC = - 129.58mm, EFL =-250mm P/N: PBB-10-R03-N129 | 1pc | 02.Jul.2008 updated |
| 1-12. | 1" xT3; Surface(S1): concave; ROC = - 155.49mm, EFL =-300mm P/N: PBB-10-R03-N155 | 2pcs | 02.Jul.2008 updated |
| 1-13. | 1" xT3; Surface(S1): concave; ROC = -259.15mm, EFL =-500mm P/N: PBB-10-R03-N259 | 2pcs | 02.Jul.2008 updated |
| 1-14. | 1" xT3; Surface(S1): concave; ROC = -518.30mm, EFL =-1000mm P/N: PBB-10-R03-N518 | 2pcs | 02.Jul.2008 updated |