SELECTION GUIDE   								       latest update date: 02 July 2008

(IN STOCK; DELIVERY IMMEDIATELY FROM SINGAPORE STOCK)

(1) 780NM HIGH REFLECTION MIRROR  - (SINGLE WAVELENGTH COATING)

(TWO-SIDE DIELECTRIC COATED)

| ITEM | PART NO./DESCRIPTIONS | IN-STOCK QUANTITY | APPLICATION/DRAWING/COATING DESCRIPTIONS |
| --- | --- | --- | --- |
| 1. | 780nm High-Reflection Mirrors(High Energy) Substrate: Fused Silica Diameter: 0.5" -0.20/+0.00; Thickness: 6.00±0.05mm Fine polished – double side: Flatness: / 10 @ 633nm over aperture Surface quality: better than 20-10 S/D coated High energy dielectric coating: 0o AOI DESIGNED Surface -1(S1): FLAT or CONCAVE R > 99.8% @ 780nm Surface -2(S2): FLAT AR @ 780nm(R<0.2%) Including: |  | S2: FLAT AR COATED @780nm HR @ 780nm R > 99.8%; 0o AOI; Center @ 780nm Designed S1: FLAT or CONCAVE THK =6mm |
| 1-1. | Surface -1(S1): flat P/N: PM-05-HR780-AR-0-P | 25pcs | 02.Jul.2008 updated |
| 1-2. | Surface -1(S1): concave; ROC = - 50mm P/N: PM-05-HR780-AR-0-N50 | 6pcs | 02.Jul.2008 updated |
| 1-3 | Surface -1(S1): concave; ROC = - 100mm P/N: PM-05-HR780-AR-0-N100 | 10pcs | 02.Jul.2008 updated |