www.photonik.com.sg

1.  Ø1" Plano-Convex Lens, with double-side AR coating of 650  ~ 1100nm

Plano-Convex Lens

Material: BK7

Diameter: 1” (25.4mm)

Diameter Tolerance(mm): +0.00/-0. 15

Focal Length Tolerance: 1% (Design Wavelength: 633nm)

Scratch/Dig:  40/20

AR Coated@650-1100nm, double-side, R<0.25%.

Focal Length(mm):

f1= 25.4mm;			f2=35 mm;			f3 =50mm;			f4 =75mm;			f5=100mm;

f6=125 mm;				f7=150mm;			f8=200mm;			f9=250mm;			f10=300mm;

f11=400mm;			f12=500mm;		f13=750mm;		f14=1000mm

2.  Ø 0.5" Plano-Convex Lens, with double-side AR coating of 650  ~ 1100nm

Plano-Convex Lens

Material: BK7

Diameter: 0.5”(12.7mm)

Diameter Tolerance(mm): +0.00/-0. 15mm

Focal Length Tolerance: 1% (Design Wavelength: 633nm)

Scratch/Dig:  40/20

AR Coated@650-1100nm, double-side, R<0.25%.

Focal Length(mm):

f1=15.0mm;				f 2= 25.4mm;			f 3=35mm;			f4 =50mm;			f 5  =75 mm;

f6=100mm;				f 7=125mm;				f 8=150mm;			f 9 =200 mm;		f 10=250mm;

f11=300mm;			f12=500mm;			f13=750mm;		f14=1000mm