1064NM FLAT & CONCAVE OUTPUT COUPLER

T =0%(HR), 0.2%, 3.5%, 5%, 7%, 8%, 9%, 11.5%, 15%, 17%, 25% @1064nm

| ITEM | QTY | PART NO./DESCRIPTIONS |  |  |
| --- | --- | --- | --- | --- |
| A. A1. A2. A3 A4 A5 A6 A7 A8 A9 A10 A11 A12 A13 A14 A15 A16 A17 A18 A19 |  | 1064nm Flat or Concave Output Coupler - Fused silica - Diameter:  12.7mm, - 0.20, +0.00 - Plano-plano OR plano-concave; fine polished double surfaces; Clear aperture: >90% - Surface quality: 20-10 scratch and dig(coated) - < /10 flatness @ 633nm over aperture - Parallelism: <3' - Coating: High energy dielectric coating S1: R% @1064nm (0o AOI) S2 (FLAT): AR @ 1064nm(R<0.1%@1064nm) - Thickness: 6 mm S1 FLAT, HR P/N: POC1064-PP-05-HR S1 FLAT, T=0.2% P/N: POC1064-PP-05-0.2 S1 FLAT, T=3.5% P/N: POC1064-PP-05-3.5 S1 FLAT, T=4% P/N: POC1064-PP-05-4 S1 FLAT, T=5% P/N: POC1064-PP-05-5 S1 FLAT, T=7% P/N: POC1064-PP-05-7 S1 FLAT, T=8% P/N: POC1064-PP-05-8 S1 FLAT, T=9% P/N: POC1064-PP-05-9 S1 FLAT, T=10% P/N: POC1064-PP-05-10 S1 FLAT, T=15% P/N: POC1064-PP-05-15 S1 FLAT, T=17% P/N: POC1064-PP-05-17 S1 FLAT, T=25% P/N: POC1064-PP-05-25 ----------------------------- S1 CONCAVE(ROC = -900mm), HR P/N: POC1064-PCV-05-HR-N900 S1 CONCAVE(ROC = -900mm), T=0.2% P/N: POC1064-PCV-05-0.2-N900 S1 CONCAVE(ROC = -900mm), T=3.5% P/N: POC1064-PCV-05-3.5-N900 S1 CONCAVE(ROC = -900mm), T=4% P/N: POC1064-PCV-05-4-N900 S1 CONCAVE(ROC = -900mm), T=5% P/N: POC1064-PCV-05-5-N900 S1 CONCAVE(ROC = -900mm), T=7% P/N: POC1064-PCV-05-7-N900 S1 CONCAVE(ROC = -900mm), T=11.5% P/N: POC1064-PCV-05-11.5-N900 | ## R@1064nm | ## AR @1064nm Thk=6mm S2: FLAT S1: FLAT OR CONCAVE |