1064NM FLAT OUTPUT COUPLER   (R 75%)

P/N: POC1064-PP-05-25

| ITEM | QTY | PART NO./DESCRIPTION |  |  |
| --- | --- | --- | --- | --- |
| A. A1. A2. |  | 1064nm Flat Output Coupler (R=75%) - Fused silica - Diameter: ( 12.7mm, - 0.20, +0.00 - Plano-plano; fine polished double surfaces - Surface quality: 20-10 scratch and dig - < (/10 flatness @ 633nm over 5mm area - Parallelism: <3' - Coating: High energy dielectric coating S1: R=75% @1064nm (0o AOI) S2: AR @ 1064nm(R<0.1%@1064nm) Thickness & Quantity, including: Thickness: 9.52mm P/N: POC1064-PP-05-25-0.37 Thickness: 6 mm P/N: POC1064-PP-05-25-0.24 |  |  |

# Text boxes

Thk=6mm

## AR

@1064nm

## AR

@1064nm

## R=75%

@1064nm

## R=75%

@1064nm

Thk=9.52mm